Non covalent immobilization of pyrene-tagged ruthenium complexes onto graphene surfaces for recycling in olefin metathesis reactions

Houssein Nasrallah,a Stéphane Germain,b Pierre Queval,b Caroline Bouvier,a

Marc Mauduit,b Christophe Crévisyb* and Emmanuelle Schulza*

aInstitut de Chimie Moléculaire et des Matériaux d’Orsay, CNRS UMR 8182, Université Paris-Sud,

Université Paris-Saclay, bâtiment 420, 91405 Orsay cedex, France

00 33 1 69 15 73 56, emmanuelle.schulz@u-psud.fr

bEcole Nationale Supérieure de Chimie de Rennes, CNRS UMR 6226, 11 allée de Beaulieu, CS 50837,

35708 Rennes cedex 7, France

00 33 2 23 23 80 74, christophe.crevisy@ensc-rennes.fr

CONTENT

Kinetic profile in the homogeneous ene-yne RCM of S2 and the RCM of S3 with C1 and C2.

Study of the stability of C3 in CDCl3 solution by 1H-NMR.

UV-Visible spectra for the immobilization of C1, C2, C3 and L.

Description of the determination by GC analysis for S1 (with pentadecane as internal standard), S2 and S3. Copy of representative chromatograms.

Copy of 1H- and 13C-NMR spectra.

Kinetic profile in the homogeneous ene-yne RCM of S2 and the RCM of S3 with C1 and C2.

Kinetic profiles of DEDAM (S1) metathesis using C2 as catalyst. Conditions : [DEDAM]=0.2 M, toluene-D8, yield determined by NMR 1H spectroscopy using mesitylene as internal standard. A) [C2]=250 ppm, 60 °C, B) [C2]=100 ppm, 60 °C, C) [C2]=500 ppm, rt.

Kinetic profiles of S1, S2 and S3 metathesis using C1 as catalyst. Conditions : [Sx]=0.2 M, toluene-D8, 60 °C, yield determined by NMR 1H spectroscopy using mesitylene as internal standard.

Kinetic profiles of S1, S2 and S3 metathesis using C2 as catalyst. Conditions : [Sx]=0.2 M, toluene-D8, 60 °C, yield determined by NMR 1H spectroscopy using mesitylene as internal standard.

Study of the stability of C3 in CDCl3 solution by 1H-NMR

Study of the stability of C3 in CDCl3 solution by 1H-NMR spectroscopy. Conditions : [C3]0 = 32 mM, 1,1,2,2-tetrachloroethane (internal standart) 16 mM, CDCl3 500 μL, 60 °C. Degradation mesured by integrating Ru=CH signal against internal standard.

UV-Visible spectra for the immobilization of C1, C2 , C3 and L

UV-Vis Spectra for the immobilization of C1 on rGO, in DCM, room temperature, C1/rGO = 1/20, t(min)

UV-Vis Spectra for the immobilization of C2 on rGO, in DCM, room temperature, C2/rGO = 1/20, t(h).

UV-Vis Spectra for the immobilization of C3 on rGO, in DCM, room temperature, C3/rGO = 1/40, t(h)

UV-Vis Spectra for the immobilization of L on rGO, in DCM, room temperature, L/rGO = 1/10, t(min)

Description of the determination by GC analysis for S1 (with pentadecane as internal standard), S2 and S3. Copy of representative chromatograms

For substrate S1 : Column type: DB-23, 60m × 0.25mm, 0.25μm.

Method: 60 °C (1 min), 10 °C/min to 250 °C (5 min).

For substrate S2 : Column type: DB-23, 60m × 0.25mm, 0.25μm.

Method: 100 °C (1 min), 10 °C/min to 250 °C (15 min).

For substrate S3 : Column type: DB-23, 60m × 0.25mm, 0.25μm.

Method: 100 °C (1 min), 10 °C/min to 250 °C (15 min).

Copy of 1H- and 13C-NMR spectra